Supplementary information

Autonomous Self-Healable, Ag Nanowire-Polymer Composite Flexible Electrode for Underwater Sensors

Zhengyang Kong1†, Elvis K. Boahen1†, Hayoung Lim1, Do Hwan Kim1,2,3*

1Department of Chemical Engineering, Hanyang University, Seoul, Korea

2Institute of Nano Science and Technology, Hanyang University, Seoul, Korea

3Clean-Energy Research Institute, Hanyang University, Seoul, Korea

Fig. S1. Synthesis route of BPUs

Fig. S2. Functionalization of HTPB and synthesis route of FPU

Table S1. The componential mole ratios of various BPUs.

| Batch NO. | Components |  |  | Catalyst | Hard Segments (%) | Mw (g/mol) | PDI | Content of GBDB (wt%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | GB (g) | HTPB (g) | IPDI (ml) | DBTDL (g) |  |  |  |  |
| BPU-1 | 1.0 | 10 | 1.7 | 0.25 | 21.3 | 3.5 | 2.3 | 7.9 |
| BPU-2 | 1.5 |  | 2.2 |  | 27.0 | 3.9 | 2.4 | 10.9 |
| BPU-3 | 2.0 |  | 2.6 |  | 31.5 | 3.7 | 2.2 | 13.7 |
| BPU-4 | 2.5 |  | 3.1 |  | 35.9 | 3.5 | 2.1 | 16.0 |
| BPU-5 | 3.0 |  | 3.5 |  | 39.4 | 3.6 | 2.3 | 18.2 |

Table S2. The componential mole ratios of various BPUs.

| Sample | Tensile strength (MPa) | Elongation at break (%) | Modulus (MPa) | Toughness (MJ/m3) |
| --- | --- | --- | --- | --- |
| BPU-1 | 0.83±0.04 | 1213±9 | 0.26±0.01 | 4.36±0.34 |
| BPU-2 | 0.95±0.03 | 1132±6 | 0.30±0.01 | 5.25±0.65 |
| BPU-3 | 1.47±0.03 | 1098±9 | 0.42±0.01 | 7.81±0.52 |
| BPU-4 | 2.20±0.01 | 961±11 | 1.30±0.02 | 10.21±0.19 |
| BPU-5 | 2.61±005 | 594±5 | 0.87±0.01 | 7.45±0.23 |